Abstract for oral presentation

Developing a whole range of new hydrocolloids - the production and modification of alternan

T Thiele, V Landschütze

aevotis GmbH, Hermannswerder 20a, 14473 Potsdam, Germany

Alternan, a biopolymer consisting of alpha 1,3-alpha-1,6 glycosidic linkages, was described in 1982 by Côté and Robyt1 - but there is no alternan commercially available until today. For the scale-up of alternan production an optimisation of the bioconversion was conducted and several purification methods were screened consecutively. Additionally the purified alternan was used as a basis for several chemical modifications.

Sucrose is the raw material for the bioconversion of alternan. In addition to the release of fructose during bioconversion leucrose and alternan-oligosaccharides are formed as by-products. By changing the process conditions a yield of 30 % based on dry matter was achieved. The resulting alternan has a high molecular mass of 40 x 106 g/mol and a diameter of 50 nm.

Despite the high molar mass the viscosity of alternan solutions is quite low at concentrations lower than 15 %. To increase the viscosity and to broaden the range of potential applications chemical modification of alternan was tested. By carboxymethylation the viscosity was increased up to a factor of 10.000. After introduction of hydrophobic groups to the alternan backbone, the resulting alternan-esters show emulsifying properties.

The production and modification of alternan was developed on pilot scale and can be scaled-up easily for industrial applications. As oligosaccharides produced by alternansucrase are already self-affirmed GRAS the use of alternan and its modifications for food applications should be possible.

References:

1	Côté G.L., and Robyt. (1982) Isolation Isolation and partial characterization of an extracellular glucansucrase from Leuconostoc mesenteroides NRRL B-1355 that synthesizes an alternating (1  6), (1  3)-alpha-D-glucan. Carbohydrate Research 101(1). 57-74.